ISLAMIC UNIVERSITY OF TECHNOLOGY

(A subsidiary organ of OIC)

A STUDY TO ASSESS THE SUITABILITY OF USING POLYPROPYLENE IN CONCRETE AS A PARTIAL REPLACEMENT OF COARSE AGGREGATE

PRESENTED BY

A.S.M.SAYEM (105415)

FAHMID TOUSIF (105422)

ABUL HASNAT (105428)

SUPERVISED BY

DR. MD JAHIDUL ISLAM

ASSISTANT PROFESSOR

DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING (CEE)

ISLAMIC UNIVERSITY OF TECHNOLOGY (IUT)

BOARD BAZAR, GAZIPUR, BANGLADESH.

NOVEMBER, 2014

# APPROVAL

THIS IS TO CERTIFY THAT THE THESIS SUBMITTED BY A.S.M.SAYEM, FAHMIDTOUSIF AND ABUL HASNAT ENTITLED AS “A STUDY TO ASSESS THE SUITABILITY OF USING POLYPROPYLENE IN CONCRETE AS A PARTIAL REPLACEMENT OF COARSE AGGREGATE” HAS BEEN APPROVED, IN PARTIAL FULFILLMENT OF THE REQUIREMENTS FOR THE BACHELOR OF SCIENCE DEGREE IN CIVIL AND ENVIRONMENTAL ENGINEERING.

SUPERVISOR

Dr. Md. Jahidul Islam

Assistant Professor

Department of Civil and Environmental Engineering (CEE)

Islamic University of Technology (IUT)

Board Bazar, Gazipur, Bangladesh.

# DECLARATION

WE HEREBY DECLARE THAT THE UNDERGRADUATE RESEARCH WORK REPORTED IN THIS THESISHAS BEEN PERFORMED BY US UNDER THE SUPERVISION OF DR. MD. JAHIDUL ISLAM AND THIS WORK HAS NOT BEEN SUBMITTED ELSEWHEREFOR ANY PURPOSE(EXCEPT FOR PUBLICATION).

A.S.M.Sayem (105415)

FahmidTousif(105422)

AbulHasnat(105428)

DEDICATED

TO

OUR PARENTS

# ACKNOWLEDGEMENT

ALL PRAISES TO ALMIGHTY ALLAH (SWT) WHO HAS GIVEN US THE OPPORTUNITY TO CONDUCT THIS RESEARCH WORK. OUR GRATITUDE AND RESPECT TO OUR SUPERVISOR DR. MD. JAHIDUL ISLAM, ASSISTANT PROFESSOR, DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING (CEE), ISLAMIC UNIVERSITY OF TECHNOLOGY (IUT) FOR HIS PATIENCE,ENCOURAGEMENT ANDJUDICIOUS ADVICES THROUGHOUT THE COURSE FOR ESTABLISHING SUCH A CREATIVE RESEARCH. IN ADDITION, THANKS TO ASSISTANT PROFESSOR MOHAMMED SHAFIQUALALAM, WHO INTRODUCED US TO STRUCTURAL ANALYSIS, AND WHOSE PASSION FOR THE “STRUCTURE” HAD LONG LASTING EFFECT ON US.WE ARE USING THIS OPPORTUNITY TO EXPRESS OUR GRATITUDE TO EVERYONE OF CEE’10, WHO SUPPORTED US THROUGHOUT THE JOURNEY. WE ARE THANKFUL FOR THEIR INVALUABLY CONSTRUCTIVE CRITICISM AND FRIENDLY ADVICE DURING THE RESEARCH WORK & THE RESEARCH ITSELF FOR LETTING US EXPERIENCING THE STIMULATING DISCUSSIONS, THE SLEEPLESS NIGHTS WE WERE WORKING TOGETHER BEFORE DEADLINES, AND ALL THE FUN WE HAVE HAD IN THE LAST ONE YEAR. GETTING THROUGH OURTHESIS REQUIRED MORE THAN ACADEMIC SUPPORT, AND WE HAVE MANY, MANY PEOPLE TO THANK FOR LISTENING TO AND, AT TIMES, HAVING TO TOLERATE US OVER THE PAST FOURYEARS SPECIALLY SALAMAHMEHERIEROVIK (CEE’09) VAI FOR HIS ENORMOUS SUPPORT. MOST IMPORTANTLY, NONE OF THIS COULD HAVE HAPPENED WITHOUT SUPPORT FROM OUR FAMILY.

# ABSTRACT

AMONG THE WASTE POLYMERIC MATERIALS, WHICH ARE USED IN BANGLADESH, POLYPROPYLENE (PP) IS A NOTABLE ONE DUE TO ITS EXTENSIVE USE IN THE PRODUCTION OF PLASTIC FURNITURES, NECESSARY UTENSILS, TOYS, BUCKETS, DOORS ETC. DUE TO ITS NON-BIODEGRADABLE NATURE, WITH A VISION OF RECYCLING THEM, A PROCESS OF CONVERTING THEM INTO LOW DENSITY PLASTIC COARSE AGGREGATE CAN BE INTRODUCED BY MELTING & COOLING THEM INTO THE MOLDS. IN THIS STUDY, THESE LOW DENSITY PLASTIC COARSE AGGREGATES HAVE BEEN USED TO PARTIALLY REPLACE THE CONVENTIONAL COARSE AGGREGATE (BRICK CHIPS) BY 10%, 20% & 30% BY VOLUME. WATER CEMENT RATIOS OF 0.42, 0.48 & 0.57 HAVE BEEN SELECTED TO ASSESS DIFFERENT PROPERTIES OF THE CONCRETE. HAVING THE MIX PROPORTION OF 1:1.5:3 (CEMENT: FINE AGGREGATE: COARSE AGGREGATE), COMPRESSIVE STRENGTH, TENSILE STRENGTH & OTHER PROPERTIES OF THE CONCRETE CYLINDERS HAVE BEEN INVESTIGATED AT 28 DAYS, FOR THREE REPLACEMENT RATIOS AS WELL AS THREE WATER CEMENT RATIOS TO COMPARE THEM WITH THE REGULAR CONCRETE (RC). THE RESULTS DEMONSTRATED THAT PP HAS BETTER BONDING CAPACITY THAN BRICK CHIPS, INCREASING THE COMPRESSIVE STRENGTH & TENSILE STRENGTH OF THE POLYPROPYLENE COARSE AGGREGATE CONCRETE (PCA CONCRETE). THUS, THIS LOW DENSITY CONCRETE CAN BE USED FOR THE STRUCTURAL PURPOSES.

KEYWORDS: POLYPROPYLENE, LIGHTWEIGHT CONCRETE, COMPRESSIVE STRENGTH, TENSILE SPLITTING STRENGTH 
TABLE OF CONTENTS

TITLE											PAGE

APPROVAL										II

DECLERATION									III

DEDICATION										IV

ACKNOWLEDGEMENT								V

ABSTRACT										VI

CHAPTER ONE: INTRODUCTION						1

  - GENERAL									1

1.2 LITERATURE REVIEW							2

1.3 OBSERVATIONS FROM LITERATURE REVIEW			9

1.4 OBJECTIVES									10

1.5 SCOPE OF WORK								10

1.6 ORGANIZATION OF THE THESIS					11

CHAPTER TWO: METHODOLOGY						12

2.1 INTRODUCTION								12

2.2 SPECIFIC GRAVITY							12

2.2.1 BASIC PROCEDURE FOR

COARSE AGGREGATE						14

2.2.2 BASIC PROCEDURE FOR

FINE AGGREGATE						14

2.3 SLUMP TEST									14

2.4 CASTING AND CURING							15

2.5 COMPRESSIVE STRENGTH TEST					16

2.6 TENSILE SPLITTING STRENGTH TEST				16

2.7 DENSITY MEASUREMENT OF AGGREGATE			17

2.7.1 BASIC PROCEDURE FOR

FINE AGGREGATE						17

2.7.2 BASIC PROCEDURE FOR

COARSE AGGREGATE						18

2.8 MIX DESIGN									18

2.9 FAILURE PATTERN OF CONCRETE					19

CHAPTER THREE: MATERIALS FOR CONCRETE			22

3.1 GENERAL									22

3.2 BINDING MATERIAL							23

3.3 COARSE AGGREGATE							24

3.3.1 BRICK AGGREGATE						24

3.3.2 PLASTIC AGGREGATE						27

3.4 FINE AGGREGATE								31

3.5 CONCLUSION									34

CHAPTER FOUR: RESULTS AND DISCUSSION				35

4.1 GENERAL									35

4.2 WORKABILITY								35

4.3 DENSITY									37

4.4 COMPRESSIVE STRENGTH						39

4.5 TENSILE STRENGTH							41

4.6 FAILURE PATTERN								42

4.7 CONCLUSION									42

CHAPTER FIVE: CONCLUSION AND RECOMMENDATIONS		43

5.1 GENERAL									43

5.2 SUMMARY AND CONCLUSION						43

5.3 RECOMMENATIONS							43

REFERENCES										45

APPENDIX										47

LIST OF TABLES

TABLE 2. 1 MIX DESIGN OF CONCRETE 					19

TABLE 3.1 CHEMICAL COMPOSITION OF BINDING MATERIAL 	23

TABLE 3.2 PROPERTIES OF BINDING MATERIAL				24

TABLE 3.3 PROPERTIES OF COARSE AGGREGATE (BRICK)		25

TABLE 3.4 FM CALCULATION OF BRICK CHIPS				25

TABLE 3.5 UNIT WEIGHT AND ABSORPTION CAPACITY

OF BRICK CHIPS							26

TABLE 3.6 SPECIFIC GRAVITY OF BRICK CHIPS				26

TABLE 3.7 TYPICAL PROPERTIES OF PP					28

TABLE 2.8 PROPERTIES OF PCA							29

TABLE 2.9 FM CALCULATION OF PP						29

TABLE 2.10 UNIT WEIGHT AND ABSORPTION CAPACITY OF PP	30

TABLE 2.11 SPECIFIC GRAVITY OF PP 					30

TABLE 3.12 PROPERTIES OF FINE AGGREGATE (SYLHET SAND)	32

TABLE 3.13 FM CALCULATION OF SYLHET SAND				32

TABLE 3.14 SPECIFIC GRAVITY AND ABSORPTION CAPACITY

OF SYLHET SAND							33

TABLE 3.15 UNIT WEIGHT OF SYLHET SAND				33

TABLE 4.1 SLUMP VALUES FOR REGULAR CONCRETE AND

PP REPLACED CONCRETE						36

LIST OF FIGURES

FIGURE 2.1 FAILURE PATTERN OF CONCRETE CYLINDER		20

FIGURE 3.1: FINENESS MODULUS OF COARSE AGGREGATE

(BRICK CHIPS)							27

FIGURE 3.2: LIGHTWEIGHT COARSE AGGREGATE

(POLYPROPYLINE)						27

FIGURE 3.3: FINENESS MODULUS OF LIGHTWEIGHT

COARSE AGGREGATE (PP)					31

FIGURE 3.4: FINENESS MODULUS OF OF FINE AGGREGATE

(SYLHET SAND)							34

FIGURE 4.1 DENSITY OF REGULAR AND PCA CONCRETE 		37

FIGURE 4.2 VARIATION IN DENSITY AND W/C RATIO OF RC

AND PCA CONCRETE						38

FIGURE 4.3 COMPRESSIVE STRENGTH TO DENSITY RATIO OF REGULAR CONCRETE AND PCA CONCRETE		38

FIGURE 4.4 TENSILE STRENGTH TO DENSITY RATIO OF

REGULAR CONCRETE AND PCA CONCRETE 		39

FIGURE 4.5 COMPRESSIVE STRENGTH (28 DAYS) OF REGULAR CONCRETE AND PCA CONCRETE 				40

FIGURE 4.6 TENSILE STRENGTH (28 DAYS) OF REGULAR

CONCRETE AND PCA CONCRETE 				41

FIGURE 4.7 FAILURE PATTERN OF RC AND PCA CONCRETE 	42